# Supporting Information: Canonical Defect Models Used for BaTiO3

## S1. Purpose and scope of the model

Canonical defect models were used to interpret the relative changes in defect chemistry among the BaTiO3 samples. The model follows the general BaTiO3 defect-chemical framework developed from prior studies of intrinsic, nonstoichiometric, acceptor-doped, and donor-doped BaTiO3 [1-3,16]. The model was not intended to provide a complete atomistic description of every defect complex in the experimental ceramics. Instead, it provides a constrained defect-chemical framework for comparing the four experimental compositions under the same thermal and atmospheric conditions.

The calculated defect chemistry was obtained by first equilibrating all defect species included in the model at 1150 °C and then calculating the low-temperature state at 500 °C. The cation vacancy concentrations were frozen from the 1150 °C equilibrium state, while electronic carriers, oxygen vacancies, and Mn redox states were allowed to re-equilibrate at 500 °C as a function of oxygen partial pressure. This treatment approximates the fact that cation diffusion is slow during cooling, whereas oxygen exchange and electronic redistribution remain more accessible over the temperature range relevant to the impedance measurements.

## S2. Defect species and notation

The following species were included in the models:

| Symbol in model | Kröger-Vink interpretation |
| --- | --- |
| n | Electron concentration |
| p | Hole concentration |
| VO∙∙ | Oxygen vacancy |
| VBa'' | Barium vacancy |
| VTi'''' | Titanium vacancy |
| MnTi× | Mn4+ on Ti site |
| MnTi' | Mn3+ on Ti site |
| MnTi'' | Mn2+ on Ti site |
| YBa∙ | Y3+ on Ba site |
| A' | background acceptor |

## S3. Defect equilibria

### S3.1 Intrinsic electronic disorder

The electron-hole equilibrium was written as

nil= e'+h∙

with

Ki=np

p=Ki / n

Ki=8.55e44 exp⁡(-2.91/kT)

The same Ki was used for all compositions.

### S3.2 Oxygen reduction equilibrium

The oxygen reduction reaction was written as

OO×=VO∙∙+2e'+1/2O2(g)

with the concentration-based mass-action expression

KR=VO∙∙n2(pO2)1/2

VO∙∙=KR / (n2(pO2)1/2)

Two effective values of KR were used:

| Composition | KR expression |
| --- | --- |
| undoped BaTiO3 | KR=2.56e71 exp(-6.10/kT) |
| Mn-containing BaTiO3 | KR=1.06e71 exp(-5.69/kT) |

The reason for using two KR values is discussed in Section S5.

### S3.3 Schottky disorder and cation nonstoichiometry

For stoichiometric A/B = 1 compositions, Schottky disorder was represented as

nil=VBa''+VTi''''+3VO∙∙

with

KS=VBa''VTi''''[VO∙∙]3

KS=3.4e105 exp(-2.795/kT)

For A/B = 1, the model assumed VBa''=VTi''''. Combining the Schottky equilibrium with the oxygen reduction expression gives

VBa''=VTi''''=(KS / KR3)n3(pO2)3/4

For Ti-rich compositions with A/B < 1, the A-site vacancy concentration was fixed by the nominal cation ratio:

VBa''=(1-A/B)NB

VTi''''=0

Thus A/B = 0.999 gives VBa''=1.55e19 cm-3, and A/B = 0.994 gives VBa''=9.30e19 cm-3.

### S3.4 Mn redox equilibria

Mn was assumed to occupy the Ti site and to access Mn4+,  Mn3+, and Mn2+ charge states. The two electron exchange reactions were

MnTi'=MnTi×+e'

MnTi''=MnTi'+e'

with

KMn43=nMnTi× / [MnTi']=3.2e22 exp(-1.84/kT)

KMn32=nMnTi' / [MnTi'']=0.8e22 exp(-1.25/kT)

The total Mn concentration was fixed at 7.7e19 cm-3 for the Mn-doped and Mn+Y co-doped compositions. The Mn site balance was

[Mntotal]=MnTi×+MnTi'+[MnTi'']

For a given electron concentration n, the Mn partitioning was calculated as

MnTi'=[Mntotal] / (KMn43/n +1+n/KMn32)

MnTi''=MnTi'n / KMn32

MnTi×=Mntotal-MnTi'-MnTi''

### S3.5 Y donor concentration

For the Mn+Y co-doped composition, Y was treated as a fixed donor on the Ba site:

YBa∙=Ytotal=7.7e19 cm-3

This treatment follows the donor-acceptor compensation picture for Mn+Y co-doped BaTiO3, in which Y_Ba* provides a donor reservoir while the multivalent Mn acceptor changes charge state with oxygen activity and Fermi level position [14,15].

### S3.6 Background acceptor

For undoped BaTiO3, a small background acceptor concentration of 100 ppm was included, giving [A'] = 1.55e18 cm^-3. This term accounts for residual acceptor impurities in nominally undoped BaTiO3 and avoids treating the commercial starting powder as an ideal intrinsic crystal. The use of a small extrinsic acceptor background is consistent with prior treatments of nonstoichiometry and impurity compensation in nominally undoped BaTiO3 [1-3,7,8].

## S4. Charge neutrality and numerical solution

The charge neutrality condition was

n+2VBa''+4VTi''''+MnTi'+2MnTi''+A'=p+2VO∙∙+[YBa∙]

For each value of pO2, the equation was solved numerically for n in log10(n) space. Once n was obtained, p, VO∙∙, VBa'', VTi'''', and the Mn charge-state populations were calculated from the mass-action and site-balance expressions above.

The pO2 grid used for the defect diagrams ranged from 1e-20 to 1e5 atm. The reported air values were calculated at pO2 = 0.21 atm, not by interpolation from the grid.

## S5. Rationale for using composition-dependent effective KR values

For an ideal defect reaction written in terms of activities, the oxygen-reduction equilibrium constant is fixed by the standard-state thermodynamics of the reaction at a given temperature [16]. In the present canonical model, oxygen reduction is instead represented using the concentration-based expression

KR=VO∙∙n2(pO2)1/2.

Because this expression does not explicitly include activity coefficients, dopant-vacancy association, local charge compensation, space-charge effects, or carrier trapping, the fitted KR should be interpreted as an effective reduction constant. It is therefore not a universal thermodynamic constant, but a parameter that also contains nonideal interactions omitted from the simplified mass-action expression.

The use of two effective K_R values is not intended to assign a separate oxygen-reduction constant to every compositional change. Compositional effects that are directly represented in the model, including A/B nonstoichiometry, the background acceptor concentration, Mn redox equilibria, and the Y donor concentration, are treated explicitly. Mn is treated differently because it introduces redox-active defect chemistry coupled directly to oxygen vacancy formation. Prior weight-change, valence-state, transport, nonstoichiometry, and spectroscopic studies show that Mn-doped BaTiO3 differs from nominally undoped BaTiO3: Mn valence changes with pO2, oxygen nonstoichiometry is modified, and carriers generated by oxygen vacancy formation can be locally trapped by Mn-related states [6,9-13]. First-principles and ESR results further indicate that oxygen vacancies are stabilized near Mn and that the released electrons occupy Mn 3d states [13]. These local association and trapping effects are not explicitly captured by the canonical Mn redox equations, so they are incorporated into the Mn-bearing effective K_R.

The model therefore uses one effective K_R for nominally undoped BaTiO3 and one Mn-bearing effective K_R for both Mn-doped and Mn+Y co-doped BaTiO3. The Mn+Y composition uses the same Mn-bearing K_R because Y is included separately as a fixed donor, Y_Ba*, in the charge-neutrality condition. This keeps the model constrained while separating Mn-related oxygen-reduction behavior from the donor-acceptor compensation effect of Y, consistent with the Fermi-level-pinning picture reported for Mn+Y co-doped BaTiO3 [14,15].

## S6. Equilibrium constants used in the models

| Constant | Expression | Used for | Source / basis |
| --- | --- | --- | --- |
| Ki | 8.55e44 exp(-2.91/kT) | all compositions | canonical BaTiO3 electronic disorder framework [1-3] |
| KS | 3.4e105 exp(-2.795/kT) | all compositions | canonical BaTiO3 Schottky disorder framework [1-3] |
| KR,undoped | 2.56e71 exp(-6.10/kT) | undoped BaTiO3 | undoped effective reduction behavior; numerical form associated with BaTiO3 reduction constants from Daniels/Härdtl-type defect models [4,5] |
| KR,Mn | 1.06e71 exp(-5.69/kT) | Mn-doped and Mn+Y co-doped BaTiO3 | Mn-bearing effective reduction behavior; numerical form follows the Nowotny/Rekas general BaTiO3 reduction constant [1,2], with Mn-specific interpretation supported by Mn redox and vacancy-interaction studies [6,9-13] |
| KMn43 | 3.2e22 exp(-1.84/kT) | Mn-doped and Mn+Y co-doped BaTiO3 | Mn4+/Mn3+ redox equilibrium and Mn valence-state framework [6,9-11] |
| KMn32 | 0.8e22 exp(-1.25/kT) | Mn-doped and Mn+Y co-doped BaTiO3 | Mn3+/Mn2+ redox equilibrium and Mn valence-state framework [6,9-11] |

## S7. Code availability and reproducibility

The model equations were implemented in Python. The model is contained in `src/batio3_defects/solver.py`. The defect diagrams corresponding to the manuscript Figure 6 are generated by

python scripts/plot_figure6_defect_concentrations.py

This script writes the plotted data to `results/figure6_defect_concentrations_data.csv` and the figure files to `figures/figure6_defect_concentrations.png`, `.pdf`, and `.svg`.

## References

1. J. Nowotny and M. Rekas, "Defect chemistry of BaTiO3," Solid State Ionics 49, 135–154 (1991). https://doi.org/10.1016/0167-2738(91)90079-Q

2. J. Nowotny and M. Rekas, "Defect structure, electrical properties and transport in barium titanate. VI. General defect model," Ceramics International 20, 257–263 (1994). https://doi.org/10.1016/0272-8842(94)90060-4

3. H.-I. Yoo, C.-R. Song, and D.-K. Lee, "BaTiO3−δ: Defect structure, electrical conductivity, chemical diffusivity, thermoelectric power, and oxygen nonstoichiometry," Journal of Electroceramics 8, 5–36 (2002). https://doi.org/10.1023/A:1015570717935

4. J. Daniels and K. H. Härdtl, "Electrical conductivity at high temperatures of donor-doped barium titanate ceramics. I," Philips Research Reports 31, 489–504 (1976).

5. J. Daniels, "Electrical conductivity at high temperatures of donor-doped barium titanate ceramics. II," Philips Research Reports 31, 505–515 (1976).

6. H. J. Hagemann and D. Hennings, "Reversible weight change of acceptor-doped BaTiO3," Journal of the American Ceramic Society 64, 590–594 (1981). https://doi.org/10.1111/j.1151-2916.1981.tb10223.x

7. N.-H. Chan, R. K. Sharma, and D. M. Smyth, "Nonstoichiometry in undoped BaTiO3," Journal of the American Ceramic Society 64, 556–562 (1981). https://doi.org/10.1111/j.1151-2916.1981.tb10325.x

8. D.-K. Lee and H.-I. Yoo, "Oxygen nonstoichiometry of undoped BaTiO3−δ," Solid State Ionics 144, 87–97 (2001). https://doi.org/10.1016/S0167-2738(01)00967-5

9. H. J. Hagemann and H. Ihrig, "Valence change and phase stability of 3d-doped BaTiO3 annealed in oxygen and hydrogen," Physical Review B 20, 3871–3878 (1979). https://doi.org/10.1103/PhysRevB.20.3871

10. C.-R. Song, H.-I. Yoo, and J. Y. Kim, "Mn-doped BaTiO3: Electrical transport properties in equilibrium state," Journal of Electroceramics 1, 27–39 (1997). https://doi.org/10.1023/A:1009994230779

11. D.-K. Lee, H.-I. Yoo, and K. D. Becker, "Nonstoichiometry and defect structure of Mn-doped BaTiO3−δ," Solid State Ionics 154–155, 189–193 (2002). https://doi.org/10.1016/S0167-2738(02)00427-7

12. S.-H. Yoon, C. A. Randall, and K.-H. Hur, "Difference between resistance degradation of fixed valence acceptor (Mg) and variable valence acceptor (Mn)-doped BaTiO3 ceramics," Journal of Applied Physics 108, 064101 (2010). https://doi.org/10.1063/1.3480992

13. S. Chikada, T. Kubota, A. Honda, S. Higai, Y. Motoyoshi, N. Wada, and K. Shiratsuyu, "Interactions between Mn dopant and oxygen vacancy for insulation performance of BaTiO3," Journal of Applied Physics 120, 142122 (2016). https://doi.org/10.1063/1.4963381

14. Y. Y. Yeoh, H. Jang, and H.-I. Yoo, "Defect structure and Fermi-level pinning of BaTiO3 co-doped with a variable-valence acceptor (Mn) and a fixed-valence donor (Y)," Physical Chemistry Chemical Physics 14, 1642–1648 (2012). https://doi.org/10.1039/C2CP22711H

15. C.-E. Lee, S.-H. Kang, D.-S. Sinn, and H.-I. Yoo, "Co-doping effect of Mn and Y on charge and mass transport properties of BaTiO3," Journal of Electroceramics 13, 785–791 (2004). https://doi.org/10.1007/s10832-004-5193-9

16. J. Maier, Physical Chemistry of Ionic Materials: Ions and Electrons in Solids, Wiley, Chichester (2004). https://doi.org/10.1002/0470020229